## Slide 1: ALGINATE
Irreversible Hydrocolloid Impression Material

## Slide 2: Lesson Plan
Target audience – I BDS
Duration of lecture – 40 minutes
10 minutes – Discussion
10 minutes – Assessment using MCQs

## Slide 3
In the last century, a chemist from Scotland extracted algin from seaweeds, which was later named as anhydro-β-d-mannuronic acid. It is also called as alginic acid.
It has been in use since World War II due to the shortage of agar.
Factors responsible for its success are:
  Easy to manipulate
  Comfortable for patient
  Relatively inexpensive

## Slide 4: Composition
Component | Percentage by weight | Function
Potassium alginate | 15 | Soluble alginate
Calcium sulfate | 16 | Reactor
Zinc oxide | 4 | Filler particles
Potassium titanium fluoride | 3 | Accelerator
Diatomaceous earth | 60 | Filler particle s
Sodium phosphate | 2 | Retarder

## Slide 5: Setting Reaction
It is a sol-gel reaction where soluble alginate reacts with calcium sulfate and insoluble calcium alginate gel is formed.
This production of calcium alginate is so rapid that it does not allow sufficient working time.
Thus, trisodium phosphate is added to prolong the working time.
So, when suitable amounts of calcium sulfate, potassium alginate and trisodium phosphate are mixed the following reaction will first take place:
2Na3PO4 + 3CaSO4 Ca3(PO4)2 + 3 Na2SO4
When the supply of tricalcium phosphate (retarder) is exhausted, the calcium ions begin to react with potassium alginate to produce calcium alginate as follows:
K2nAlg + n CaSO4 n K2SO4 + CanAlg

## Slide 6
Gel Structure:
The final gel consists of a brush heap of calcium alginate fibril network enclosing unreacted sodium alginate sol, excess water, filler particles and reaction byproducts.
It is a cross-linked structure (i.e., each fiber is tied to each other at certain points).
Calcium is responsible for cross-linking.

## Slide 7: Manipulation
The powder is sifted into premeasured water that has been taken in a clean bowl.
The powder is incorporated into the water by careful mixing with a metal spatula.
A vigorous figure-eight motion is best, with the mix being swiped or stropped against the sides of the rubber mixing bowl with intermittent rotations (180 degrees) of the spatula to press out the air bubbles.
The result should be smooth, creamy mixture that does not drip off the spatula when it is raised from the bowl.
A variety of mechanical devices are also available for spatulating .

## Slide 8: Mixing Time
For fast set alginate - 45 seconds
For normal set alginate - 60 seconds
The strength can be reduced by 50 % if the mixing is not complete.
Clean equipments are important as contamination may result in too rapid a set, inadequate fluidity, or even rupture of the impression on removal from the mouth.

## Slide 9: Setting Time
Fast set alginate — 1.5 to 3 minutes
Normal set alginate: — 3-4.5 minutes
Setting time can be regulated by altering the temperature of water.
Higher the temperature the shorter is the setting time
In hot weather, special precaution should be taken to provide cool water for mixing to prevent premature gelation.
It may even be necessary to precool the mixing bowl and spatula, especially when small amounts of impression material are to be mixed.

## Slide 10: Properties
Strength:
  All manipulative factors under the control of the clinician affect the gel strength.
  Eg. i) If too little or too much water is used in mixing, the final gel will be weakened.
  ii) Insufficient spatulation results in failure of the ingredients to dissolve sufficiently so that the chemical reaction can proceed uniformly throughout the mass
  iii) Over-mixing breaks up the calcium alginate gel network as it is forming and reduce its strength.

## Slide 11
Accuracy:
Most alginates are not capable of reproducing the finer details that are observed in impressions with other elastomeric impression materials.
Dimensional Stability:
Set alginates have poor dimensional stability due to evaporation, syneresis and imbibition. Therefore, the cast should be poured immediately.
If pouring of the impression must be delayed, it should be rinsed in tap water, disinfected, wrapped in surgical paper towel, saturated with water, and placed in a sealed plastic bag or a humidor.

## Slide 12
Adhesion:
Alginate does not adhere well to the tray. Good adhesion is important for the
accuracy of the impression. Retention to the tray is achieved by mechanical
locking features in the tray or by applying an adhesive.

## Slide 13: USES
1. It is used for primary impression making
— When there are undercuts.
— In mouths with excessive flow of saliva.
— For partial dentures with clasps.
2. For impressions to make study models and working casts.
3. As duplicating materials.

## Slide 14: Advantages
1. It is easy to mix and manipulate.
2. Minimum requirement of equipment.
3. Elastic in nature
4. Accurate if properly handled
5. Relatively inexpensive
6. Comfortable to the patient
7. It is hygienic, as fresh material must be used for each impression.
8. It gives a good surface detail even in presence of saliva as it’s hydrophilic

## Slide 15: Disadvantages
1. Cannot be electroplated so metal dies are not possible
2. It cannot be corrected
3. Distortion may occur without it being obvious if the material is not held steady while it is setting.
4. Poor dimensional stability—it cannot be stored for long time.
5. Poor tear strength.
6. Because of these drawbacks and the availability of better materials, it is not recommended where a higher degree of accuracy is required. e.g., cast RPD,crowns and FPDs, etc

## Slide 16: Disinfection:
Disinfectants such as iodophor, bleach or gluteraldehyde can be used according to manufacturer’s instruction.
CDC guidelines recommend to use household bleach (1 to 10 dilution), iodophors, or synthetic phenols.
After the impression is rinsed thoroughly, the disinfectant can be sprayed liberally on the exposed surface. The impression is then wrapped immediately in a disinfectant-soaked paper towel and placed in sealed bag for 10 mins.
Then, remove the impression from the bag and shaken to remove excess water and poured.
An alternative method is to immerse, but it should not exceed 10 mins.

## Slide 17: Shelf Life
Shelf life is dependent on two factors:
  Storage temparature
  Moisture contamination
Not to store for more than 1 year
Store it in cool and dry place

## Slide 18: Laminate Technique (Alginate-agar method)
Combined agar-alginate technique
The hydrocolloid in the tray is replaced with a mix of chilled alginate that bonds with the agar expressed from the syringe.
The alginate gels by chemical reaction, whereas the agar gels by means of contact with the cool alginate.
Since the agar is in contact with the prepared teeth it records maximum details.
Indications:
  For impression of single prepared teeth
Disadvantage:
  the high viscosity of alginate may displace the agar during seating

## Slide 19
  THANK YOU